## Slide 1: Seebeck analysis

## Slide 2: Seebeck analysis
[tkprog_X_path]\electrical\Seebeck\SnSeTe-S-Hall.xlsx\

## Slide 3: Simulate
[tkprog_X_path]\electrical\Seebeck\SnSeTe-S-Hall.xlsx\
Non-degenerated
Degenerated (metal)

## Slide 4: Simulate
Non-degenerated
should be smaller => l0 should be smaller

## Slide 5: Fit
Fixed parameters:
T: Temperature
r: scattering factor
Fitting parameters:
meff: Effecitive mass
l0: Prefactor of mean free path

## Slide 6: Fit

## Slide 7: Edit prm
[Preferences]
infile=D:/tkProg/tkProg.main/tkprog_COE/electrical/Seebeck/SnSeTe-S-Hall.xlsx
T0=300.0
charge=1.0
rfac=0.5
EC=0.0
NC=7.655183943025066e+18
DC0=2.0781132532558804e+21
S2=0.09846196814223308
[Parameters]
meff=0.4531640625000002:1
l0=1.1855468750000088e-09:1

## Slide 8: Read prm
Updated the fitting parameters

## Slide 9: To get better fitting
  Edit parameter file and run ‘simulate’ to get better simulation result
  Then perform ‘fit’ for least-squares fitting
  Press ‘read prm’ to read the parameter file to the dialog
  Repeat 1 – 3 to get a good result

## Slide 10: Old documents

## Slide 11
What we can know from Seebeck measurement?
Known: , , , S
  Non-degenerated semi.
  Metal
  : Density-of-states effective mass
  (Different from carrier effective mass except for single parabolic band case (free electron model))
General case: Need simulation and fitting

## Slide 12: Seebeck.py
Purpose: Simulate Seebeck related properties based on free electron model
Model: Free electron model (Single parabolic band model) (electron only) + Boltzmann equation + relaxation time approximation
Theory: Attached in this file after usage of the program
Functions: (i) mode = ‘basic’: For debug / development purpose. Plot distribution functions and Fermi integrals (ii) mode = ‘prop’: Plot Seebeck related properties. Carrier density, mobility, conductivity, Seebeck coefficient, electron thermal conductivity, Lorentz number (ii’) mode = ‘Hall’: Plot Hall related properties. Carrier density, mobility, conductivity, Hall coefficient, Hall factor (iii) mode = ‘init’: Create .in file for the following analysis (iv) mode = ‘sim’: Calculate weighted mobility, carrier density and conductivity. Simulate Jonker / Pisarenko plots (v) mode = ‘fit’: Fit to Pisarenko plot to extract effective mass (vi) mode = ‘T’: Simulate T dependences of Seebeck-related properties (vii) mode = ‘calL’: Calculate L and κe from T, Ne data (viii) mode = ‘calF’: Calculate Fhall, NHall and drift from T, NeHall and Hall data

## Slide 13: Seebeck.py
Program: [data-COE]\Seebeck\Seebeck.py
[Programs]\python\electrical\Seebeck\Seebeck.py
Data folder: [data-COE]\SnSeTe-S-Hall.xlsx
Input files: Data file (.xlsx / .csv)
Parameter file (.in) (created by mode = ‘init’, ‘sim’ and ‘fit’))
Output files: parameter file (.in), CSV files
(i) python Seebeck.py basic
Plot basic functions
(ii) python Seebeck.py prop T meff r l0 kappa_latt
meff in me0, l0 in m, kappa_latt in W/m/K
Plot Seebeck related properties
ex: python Seebeck.py basic 300.0 0.39111328125000017 0.5 1e-08 5.0
(ii') python Seebeck.py Hall T meff r l0
Plot Hall related properties
ex: python Seebeck.py Hall 300.0 0.39111328125000017 0.5 1e-08
(iii) python Seebeck.py init infile
Create .in file
(iv) python Seebeck.py sim infile T meff r l0
Calculate weight mobility etc from input file
Plot Jonker / Pisarenko plots
ex: python Seebeck.py sim SnSeTe-S-Hall.xlsx 300.0 0.39111328125000017 0.5 1e-08
(v) python Seebeck.py fit T meff r l0
Fit to Jonker / Pisarenko plots
ex: python Seebeck.py fit SnSeTe-S-Hall.xlsx 300.0 0.39111328125000017 0.5 1e-08
(vi) python Seebeck.py T infile Tmin Tmax nT
Simulate T dependences
ex: python Seebeck.py fit SnSeTe-S-Hall.xlsx 300.0 800.0 6
(vii) python Seebeck.py calL infile meff r l0
Calculate L and kappa,e from Ne and sigma
ex: python Seebeck.py calL SnSeTe-S-Hall.xlsx 0.39111328125000017 0.5 1e-08

## Slide 14: Data file (.xlsx / .csv)
[data-COE]\Seebeck\SnSeTe-S-Hall.xlsx, SnSeTe-S-Hall.csv
The order of the data columns are arbitrary.
The data types are judged by the key words in the first line labels.
Sample specification : Any numbers.
Label must be distinguished from the other columns.
Seebeck coefficient in μV/K : Label must start from capital ‘S’
Conductivity in S/cm : Label must start from ‘sigma’
Carrier density in cm-3 : Label must start from ‘n’
Mobility in cm2/(Vs) : Label must start from ‘mu’
Te conc, x | S (uV/K) | sigma (S/cm) | n (cm-3) | mu (cm2/Vs)
0 | 900 | 0.000640871 | 1.00E+15 | 4
0.1 | 672 | 0.032172413 | 6.77E+16 | 2.96582
0.2 | 560 | 0.230976754 | 2.54E+17 | 5.6868
0.3 | 448 | 0.563164534 | 6.97E+17 | 5.04614
0.4 | 350.98 | 2.300066702 | 1.94E+18 | 7.4
0.5 | 168 | 5.952380952 | 7.33E+18 | 5.06769

## Slide 15: Parameter file (.in)
Created by mode=‘init’, ‘sim’ and mode = ‘fit’
[Preferences]
infile=SnSeTe-S-Hall.xlsx
charge=1.0
rfac=0.5
EC=0.0
NC=7.655183943025066e+18
DC0=2.0781132532558804e+21
S2=
T0=300.0
[Parameters] key=value:opt_id
opt_id must be 1
meff=0.3:1
l0=1e-08:1

## Slide 16: Plot distribution functions and Fermi integrals
(i) python Seebeck.py basic
Input files: None
Output files: fFD.csv: Fermi-Dirac distribution functions and their approximations
Fj.csv: Fermi integrals and their approximations

## Slide 17: Plot Seebeck related properties
(ii) python Seebeck.py prop T meff r l0 kappa_latt
Effective mass, meff [me0]
Scattering factor in τ
Prefactor of mean free path, l0 [m]
Lattice thermal conductivity, κlatt [W/m/K]
Plot properties
Input files: None
Output files: properties.csv

## Slide 18: Plot Seebeck related properties: r = 0.5
python Seebeck.py prop 300.0 0.3 0.5 1e-08 5.0
Output files: properties.csv

## Slide 19: Plot Seebeck related properties: r = 0.0
python Seebeck.py prop 300.0 0.3 0.0 1e-08 5.0
Output files: properties.csv

## Slide 20: Plot Seebeck related properties: r = -0.5
python Seebeck.py prop 300.0 0.3 -0.5 1e-08 5.0
Output files: properties.csv

## Slide 21: Plot Hall related properties: r = 0.5
python Seebeck.py Hall 300 0.3 0.5 1e-8
Output files: properties.csv

## Slide 22: Plot Hall related properties: r = 0.0
python Seebeck.py Hall 300 0.3 0.0 1e-8
Output files: properties.csv

## Slide 23: Plot Hall related properties: r = 2.0
python Seebeck.py Hall 300 0.3 2.0 1e-8
Output files: properties.csv

## Slide 24: Analysis

## Slide 25: Step 0’: Delete parameter file for reset
Seebeck.py reads parameters from a parameter file (.in) if it exists.
If you restart from scratch, delete it.
C:> del Hall-SnSe.in (change the file name)

## Slide 26: Step 0: Analyze scattering factor r if possible
See 50-02-mu-T-Fit.pptx
python ..\mu-T-Fit.py fit Hall-SnSe.xlsx
Console output:
Optimized at S2= 0.0669359:
Eb : -0.00019852912 optid=1
apolyi[0] : -0.012429574 optid=1
ppolyi[0] : 0 optid=0
apolyi[1] : 0.0058160275 optid=1
ppolyi[1] : -1.5 optid=0
apolyi[2] : 0.019690371 optid=1
ppolyi[2] : 1.5 optid=0
apolyi[3] : 0 optid=0
ppolyi[3] : -1 optid=0
apolyi[4] : 0 optid=0
ppolyi[4] : 1 optid=0
T(K) mu,obs(cm2/Vs) mu,ini(cm2/Vs) mu,fin(cm2/Vs)
249.9 3.76297 3.61235 3.5679
274.4 4.06679 4.0624 4.01455
297 4 4.44804 4.4005
325 5 4.86122 4.81963
370 5.5 5.29669 5.27746
428 5.3 5.35618 5.37808
472 4.7 5.0755 5.12468
523 4.8 4.54923 4.61726
572 4.3 3.9778 4.05157
625 3.6 3.38755 3.45877
672 2.7 2.9256 2.99088

## Slide 27: File format
SnSeTe-S-Hall.xlsx

## Slide 28: Step 0’: Create and edit .in file
python Seebeck.py init SnSeTe-S-Hall.xlsx
Input file: SnSeTe-S-Hall.xlsx / SnSeTe-S-Hall.csv
Output file: SnSeTe-S-Hall.in
SnSeTe-S-Hall.in:
[Preferences]
infile=SnSeTe-S-Hall.xlsx
charge=1.0 # Check polarity of S. -1.0 for electron
rfac=0.5 # Change according to the scattering mechanism
EC=0.0
NC=4.1233891183644324e+18
DC0=1.119355150572396e+21
S2=
[Parameters]
meff=0.3:1
l0=1e-08:1

## Slide 29: Simulate Jonker / Pisarenko plots
python Seebeck.py sim infile T meff r l0
Input file, infile
Temperature, T [K]
Effective mass, meff [me0]
Scattering factor in τ
Prefactor of mean free path, l0 [m]
Input files: Data file (.xlsx / .csv)
Parameter file (.in) if exists
Output files: SnSeTe-S-Hall-Seebeck-sim.csv

## Slide 30: Step 1: Simulate Jonker / Pisarenko plots
python Seebeck.py sim SnSeTe-S-Hall.xlsx
Input files: SnSeTe-S-Hall.xlsx
Output files: SnSeTe-S-Hall-muT-sim.csv (including weighted mobility etc)

## Slide 31: Step 2: Find better fit by changing meff and l0
python Seebeck.py sim SnSeTe-S-Hall.xlsx 300 0.5 0.5 1e-09
Input files: SnSeTe-S-Hall.xlsx
Output files: SnSeTe-S-Hall-muT-sim.csv (including weighted mobility etc)

## Slide 32: Step 3: Fit to Pisarenko plot to extract m*
Ex.: python Seebeck.py fit
Usage: python Seebeck.py fit infile T meff r l0
Input file, infile
Temperature, T [K]
Effective mass, meff [me0]
Scattering factor in τ
Prefactor of mean free path, l0 [m]
Input files: Data file (.xlsx / .csv)
Parameter file (.in) if exists
Output files: SnSeTe-S-Hall-Seebeck-fit.csv
Parameter file (.in)
python Seebeck.py fit

## Slide 33: Step 4: Check mode=‘sim’ with the optimized parameters
The values of meff and l0 will be red from .in file so the are not necessary given by arguments.
python Seebeck.py sim SnSeTe-S-Hall.xlsx
Input files: SnSeTe-S-Hall.xlsx, SnSeTe-S-Hall.in
Output files: SnSeTe-S-Hall-muT-sim.csv (including weighted mobility etc)

## Slide 34: Step 5: Check properties
The values of meff and l0 will be red from .in file so the are not necessary given by arguments.
The input data file is not needed and must not be given by arguments
python Seebeck.py
Input files: SnSeTe-S-Hall.xlsx

## Slide 35: Step 6: Check properties at different T
python Seebeck.py T SnSeTe-S-Hall.xlsx 200 1000 9
Calculate properties at T from 200 to 1000 at 9 points
Input files: SnSeTe-S-Hall.xlsx
Output files: *.csv

## Slide 36: cf. Properties at different T (r = 0.0)
Note: Edit .in file to change r to 0.0 to show T dependences

## Slide 37: Data file (.xlsx / .csv): Calculate L from T, Ne and  data
[data-COE]\Seebeck\Pb05Sn05Se-T-Ne-sigma.xlsx
Require T, sigma, n data
The order of the data columns are arbitrary.
The data types are judged by the key words in the first line labels.
If more than two columns fit to the condition below, the left-most columns will be red.
Temperature in K : Label must start from T followed by [ |(|[].
Conductivity in S/cm : Label must start from ‘sigma’
Carrier density in cm-3 : Label must start from ‘n’
T(K) | sigma (S/cm) | T(K) | n (cm-3)
300 | 1.15075 | 299.698 | 3.69E+18
323.1785 | 2.1339 | 323.349 | 3.92E+18
347.6345 | 5.01065 | 347.8985 | 4.26E+18
373.159 | 9.87103 | 373.31999 | 5.57E+18
398.17 | 16.76255 | 398.31999 | 6.90E+18

## Slide 38: Calculate L from T, Ne and  data
python Seebeck.py calL Pb05Sn05Se-T-Ne-sigma.xlsx 0.3 0.0 1.0e-8
Input files: Pb05Sn05Se-T-Ne-sigma.xlsx
Output files: *.csv

## Slide 39: Data file (.xlsx / .csv): Calculate FHall from Hall data
[data-COE]\Seebeck\Hall-SnSe.xlsx
Require T, n, mu data
The order of the data columns are arbitrary.
The data types are judged by the key words in the first line labels.
If more than two columns fit to the condition below, the left-most columns will be red.
Temperature in K : Label must start from T followed by [ |(|[].
Conductivity in S/cm : Label must start from ‘sigma’
Carrier density in cm-3 : Label must start from ‘n’
Mobility in cm2/Vs : Label must start from ‘mu’
T (K) | n (cm-3) | mu(cm2/Vs) | sigma(S/cm)
249.8715 | 1.02E+14 | 3.76297 | 1.44E+09
274.44749 | 3.66E+14 | 4.06679 | 2.26E+10
297 | 1.00E+15 | 4 | 1.89E+11
325 | 2.00E+15 | 5 | 1.76E+12
370 | 8.00E+15 | 5.5 | 3.12596E+13
428 | 3.00E+16 | 5.3 | 5.21E+14

## Slide 40: Calculate FHall from Hall data
python Seebeck.py calF Hall-SnSe.xlsx 0.3 0.0 1.0e-8
Input files: Hall-SnSe.xlsx
Output files: *.csv

## Slide 41: Theory

## Slide 42
What we can know from Hall measurement?
Measured:
Conductivity: (T) Mobility: Carrier density:
Relaxation time:
, , , ,
(, )
Scattering parameter: , p
Simulation:
, , , , ,
, ,
Band structure
Density of states Free carrier absorption
: Drift mobility
: Carrier effective mass

## Slide 43
What we can know from Seebeck measurement?
Known: , , , S
  Non-degenerated semi.
  Metal
  : Density-of-states effective mass
  (Different from carrier effective mass except for single parabolic band case (free electron model))
General case: Need simulation and fitting

## Slide 44: 有効質量からわかる量
有効状態密度 スピン以外の縮退のない等方的なsバンドでは、 状態密度有効質量mdeはキャリア有効質量me*に等しい
熱速度
フェルミ速度
バースタイン・モスシフト (縮退半導体のEF)
状態密度 MCは等価なLUMOのk点の数。
移動度、伝導度
Notes: 44

## Slide 45: 平衡統計力学
平衡分布関数:各粒子の の関数 ＝＞ 平衡状態の物理量平均を求める
例： キャリア密度
(自由電子近似)
平衡状態と定常状態の違い:
平衡状態: 系の巨視的状態が時間変化しない 系の一部を取り出しても同じ巨視的状態 平衡の三条件: 力学的平衡 (F、P)、熱的平衡 (T)、化学的平衡 (μ) 詳細釣り合い: 任意の2状態の組について互いへの流れが等しい
定常状態: 開いた系で、物質、エネルギーの流れ込みと放出が常に同量で あるため、見かけ上巨視的状態が変化しない
平衡状態であれば：
・ 粒子分布、物理量の時間変化がない、空間的に均一
・ エネルギー分布の時間変化がない => 電流が流れるとJoule熱が発生する
輸送特性に対しては平衡分布関数は使えない

## Slide 46: 非平衡統計力学
・ 分布関数は各粒子の の関数
: 非平衡分布関数
・ 非平衡状態を作っている条件が無くなり、 系を静置しておけば、系は平衡状態に到達する
半導体統計、Boltzmannの輸送理論:
・ 各粒子は分布関数に関しては独立: 粒子が r, k の状態を取る確率
・ 散乱がなければ、 におけるの分布は、 における の分布が時間発展したものである
例： における 分布は における に関する分布に対応

## Slide 47: Boltzmann方程式
非平衡分布関数
Boltzmann方程式: 時間変化を3つの項に分ける
F: 外場項(ドリフト項): 時間変化が 外場によるk(t)分布だけに影響を与えた場合の項
における 分布は における () に関する分布に対応
D: 拡散項: 時間変化が定速運動による r変化だけに影響を与えた場合の項
における 分布は におけるに関する分布に対応
C: 散乱項: 外場、定速運動以外の効果。 緩和時間近似: 平衡分布関数からの変化が小さく、 非平衡状態を維持する原因がなくなったら平衡状態へ戻ると仮定:
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)
http://kenzou.michikusa.jp/StaDyn/kinetic_5.pdf

## Slide 48: Boltzmann方程式
Boltzmann方程式:
Boltzmann-Bloch方程式
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)

## Slide 49: 注：ボルツマンの輸送方程式: 全微分を取ると符号が逆転
Boltzmann equation
(, )
散乱項 拡散項 ドリフト項
外力として電場 E を考える場合
注： 前ページの式と符号が逆転
＝＞ 緩和時間近似をに適用するとつじつまが合う

## Slide 50: Boltzmann equation: Stead-state
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)
Boltzmann-Bloch equation
: group velocity  : phase velocity
Steady-state

## Slide 51: 電流－電圧特性
空間的に一様として0
: 電子が占有している状態から 非占有状態へ遷移する確率

## Slide 52: Thermoelectric properties
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)
Boltzmann-Bloch equation
: group velocity  : phase velocity
Steady-state
Non-uniform and chemical potential

## Slide 53: Calculation

## Slide 54: Electron-only Free electron model
  Energy of free electron:
  Density of states:
  Free electron density in conduction band:
  Fermi-Dirac distribution function:
  Non-dengenerated semi >>1:
  Conduction band effective density of states
EC
EF
伝導帯
E
状態密度
DC(E)
fe(E)
Chart: 
f(E)
E (eV)
EF = 0.3 eV
DOS (cm-3/eV)
1

## Slide 55
  状態密度:
  厳密解:
  : Fermi積分
  近似: 金属
  近似: 半導体
公式: キャリア密度 (自由電子近似)

## Slide 56
  ,
  Fermi-Dirac分布関数
  Fermi-Dirac分布関数の微分
  Fermi積分:
  計算方法、近似:
  ・の級数展開については「熱電変換工学」参照
  ・ x ~ 0は特異点になる(微分が発散)ので、 x = z2 の置換を行うとよい。 ただし、xが大きい領域では変数変換しないほうが速い。
  ・ 近似 ()：
  ガンマ関数:
  (nが整数)
  ,
公式: Fermi積分

## Slide 57: キャリアの散乱
平均自由行程
非縮退半導体
で代表される
縮退半導体 キャリア輸送物性にはの電子だけが寄与
で代表される
マティーセン則

## Slide 58: キャリアの散乱
/
非縮退半導体
縮退半導体 (温度に依存しない)
Heavily doped semiconductor, P.86
A model for the high-temperature transport properties of heavily doped n-type silicon-germanium alloys, JAP 69 (1991) 331 Fig. 3
 | r | τ(E,T) => τ(T)非縮退 / 縮退 | μnon-deg | μdeg
Intravalley acoustic phonons | 0 | E-1/2T-1 => T-3/2 / T-1 | T-3/2 | T-1
Intervalley optical phonons | 0 | E-1/2T-1 => T-3/2 / T-1 | T-3/2 | T-1
Ionized impurities | 2 | E3/2T0 => T3/2 / T0 | T3/2 | T0
Neutral impurities | 1/2 | E0T0 => T0 / T0 | T0 | T0
Alloy disorder | 0 | E-1/2T0 => T-1/2 / T0 | T-1/2 | T0
Optical phonon, T<<θD, high-doped & Low-doped | 1/2 |  |  | 
Optical phonon, T>>θD | 1 | T-1/2 | T0 | T0
Electron-electron scattering |  |  |  | T-2
 | r | τ(E,T) => τ(T)非縮退 / 縮退 | μnon-deg | μdeg
Intravalley acoustic phonons | 0 | E-1/2T-1 => T-3/2 / T-1 | T-3/2 | T-1
Intervalley optical phonons | 0 | E-1/2T-1 => T-3/2 / T-1 | T-3/2 | T-1
Ionized impurities | 2 | E3/2T0 => T3/2 / T0 | T3/2 | T0
Neutral impurities | 1/2 | E0T0 => T0 / T0 | T0 | T0
Alloy disorder | 0 | E-1/2T0 => T-1/2 / T0 | T-1/2 | T0
Optical phonon, T<<θD, high-doped & Low-doped | 1/2 |  |  | 
Optical phonon, T>>θD | 1 | T-1/2 | T0 | T0
Electron-electron scattering |  |  |  | T-2
Heavily doped semiconductor, P.86
A model for the high-temperature transport properties of heavily doped n-type silicon-germanium alloys JAP 69 (1991) 331 Fig. 3

## Slide 59
  キャリアの運動量緩和時間 r: 散乱因子
  (: 電気素量)
  # 速度の計算のE の単位は J, l(T,E)のE はeV で規格化するとが実際の平均自由行程に
  # 近くなる。その場合、 -r が残る (は電気素量)
  # l0 を に置き換えると、すべての E を J 単位で扱える
x = E/kT => dx = dE/kT
公式: 電気伝導度、移動度

## Slide 60
( 合金散乱では p = 0, r = ½)
Carrier density
Conductivity and Mobility
平均緩和時間

## Slide 61: 平均緩和時間
等方的な統計積分の中で置き換え:
,
から導出
他の積分表現
=> ,

## Slide 62: Hall effect
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)
When ,
=>
(q = –e for electron, +e for hole)
: Hall factor : Hall mobility
具体的な例：
  近似 ()：
  ガンマ関数:
  (nが整数)
  ,

## Slide 63: Hall因子 FHall
NC = 5.3×1018 cm-3
RH = FHall / en FHall: 散乱機構に依存

## Slide 64
q = +|e| (正孔)、-|e| (電子)
厳密解
近似: 縮退半導体: の場合
Bhattacharya et al., JAP 115, 223712 (2014)
寺崎一郎著、熱電材料の物質科学
近似: 縮退半導体:  = 0 + ((E-EF)/EF) 1 の場合
近似: 非縮退半導体 ()
真性半導体:
高温極限: 第1項はTに反比例して無視できる 寺崎一郎著、熱電材料の物質科学、内田老鶴圃 (2017)
(注意: T一定の式ではではないが、T一定でもSは一粒子当たりエントロピーと解釈できる)
=> : ホッピング伝導 (small polaron): エントロピー輸送
熱電出力
無次元性能指数
公式: 熱電関係

## Slide 65: Jonker/Pisarenkoプロット
  Jonkerプロット G.H. Jonker, Philips Res. Repts 23 (1968) 131 => 移動度が決まる
  Weighted mobility を使うと有効質量が消える
  => にかかわらずが決まる
  Pisarenkoプロット
  Pisarenko (Jonker)プロットから有効質量を求める
amorphous
数値計算値

## Slide 66: Weighted mobility
Weighted Mobility
G. Jeffrey Snyder,* Alemayouh H. Snyder, Maxwell Wood, Ramya Gurunathan,
Berhanu H. Snyder, and Changning Niu
Adv. Mater. 32 (2020) 2001537
3 % error for |S| > 20 V/K
Free electron model
Constant mean free path
(non-degenerate limit)
(degenerate limit)
Notes: 66

## Slide 67: 電子の熱伝導率: Wiedemann-Frantzの法則
キッテル固体物理学入門 第8版、丸善
気体の熱伝導率
の電子の速度はFermi速度
電子比熱
電気伝導度 (移動度 )
Wiedemann-Frantzの法則 (金属):
(非常に低温の場合を除いて) 金属の熱伝導率と電気伝導率の比は温度に比例する
: Lorenz数

## Slide 68
ref: 坂田亮、熱電変換工学, REALIZE INC
Lorenz数:
縮退極限 (Wiedemann-Frantz則):
近似式 (誤差10%)
Ref: Kim et al., APL Mater. 3, 041506 (2015)
公式: 半導体・金属の熱伝導率

## Slide 69
 | Electronic struct | Relax time τ | T dependence
ALAMODE | First-principles, Full band E = E(k) | First-principles e-ph scattering τ = τ(k) | Electron and phonon excitation with anharmonic phonon
BoltzTrap2 | First-principles, Full band E = E(k) | Constant relaxation time approximation τ(E) = τ0 | Electron and phonon excitation with anharmonic phonon
Seebeck.py | Free electron approximation, DOS (isotropic) | Energy-dependent τ(E) = τ0Er – ½ | Electron excitation. Phonon effect is included in τ(E)
EF-T_VASP.py Statistical properties only | First-principles, DOS (isotropic) |  | Electron excitation. Phonon effect is included in τr – ½
EF-T_FEA.py | Free electron approximation, DOS (isotropic) | Energy-dependent τ(E) = τ0Er – ½ | Electron excitation. Phonon effect is included in τ(E)
Hierarchy of transport simulations

## Slide 70: Mott’s formula of Seebeck coefficient
: conductivity-like function (電気伝導率的関数）
分子
分母 =
Mottの公式
=>
寺崎一郎著、熱電材料の物質科学、内田老鶴圃 (2017)

## Slide 71: 自由電子密度、自由正孔密度
  (9.41)
  非縮退半導体 >>1 では
  伝導帯有効状態密度
  同様に
  価電子帯有効状態密度
EV
EC
EF
価電子帯
伝導帯
E
状態密度
DV(E)
DC(E)
fe(E)
Chart: 
f(E)
E (eV)
EF = 0.3 eV
DOS (cm-3/eV)
1

## Slide 72: 有効質量からわかる量
有効状態密度 スピン以外の縮退のない等方的なsバンドでは、 状態密度有効質量mdeはキャリア有効質量me*に等しい
熱速度
フェルミ速度
バースタイン・モスシフト (縮退半導体のEF)
状態密度 MCは等価なLUMOのk点の数。
移動度、伝導度
Notes: 72

## Slide 73: 気体の熱伝導率
熱伝導率 K の定義: 熱流と温度勾配の比例係数
熱流 K: 熱伝導率
気体の分子運動論から比熱の式を導出:
・ 粒子が局所的な温度 の領域から の領域に進む
・ 粒子は のエネルギーを放出する : 1粒子の比熱
・ 粒子の平均自由行程 の両端における温度差 : 平均散乱時間
: x 方向の速度
熱流は時間当たりの熱の移動なので、粒子数 n と速度 に比例する
ここで、全比熱 、平均自由行程 を使って
熱伝導率 : 気体だけでなく、フォノン、電子ガスにも使える
キッテル固体物理学入門 第8版、丸善

## Slide 74: 局在電子のSeebeck係数符号反転
局在状態でのVRH伝導の場合 （拡散係数をエネルギーに対して一定とする）。 Mottの式:
ホッピングの活性化エネルギー
に等しいと仮定する
G.H. Jonker, Philips Res. Repts 23 (1968) 131
I.P. Zvyagin, Phys. Stat. Sol. B58 (1973) 443
V.V. Kosarev, Sov. Phys. – Semicond. 8 (1975) 897
H. Overhof, Pys. Stat. Sol. B67 (1975) 709
P. Butcher, in Proc. 6th ICALS (1976) p.89
「非晶質材料の電気伝導」、ネビルモット著、現代工学社、2003年第2版

## Slide 75: Other slides

## Slide 76: 移動度
GaAsの場合

## Slide 77: フォノンの散乱時間 熱電変換

## Slide 78: 熱電変換

## Slide 79: T dependence of mobility vs scat. mechanism
Acoustic photon (Non-degen.)
Acoustic photon (Degenerated)
Optical photon T<<θD, high-doped
Optical photon T<<θD, Low-doped
Ionized impurity (Non-denen.)
Neutral impurity
Heavily doped semiconductor, P.86
A model for the high-temperature transport properties of heavily doped n-type silicon-germanium alloys, JAP 69 (1991) 331 Fig. 3
Ionized impurity (Degenerated)
Notes: 79

## Slide 80: Boltzmann方程式: 散乱の緩和時間近似
平衡分布関数
非平衡分布関数
Boltzmann方程式
F: 外場項(ドリフト項): 時間変化が 外場によるk(t)分布だけに影響を与えた場合の項
=> における 分布は におけるに対応
D: ドリフト項: 時間変化が定速運動による r(t)分布だけに影響を与えた場合の項
における 分布は におけるに対応
C: 散乱項: 外場、定速運動以外の効果。 緩和時間近似: 平衡分布関数からの変化が小さく、 非平衡状態を維持する原因がなくなったら平衡状態へ戻ると仮定:
Boltzmann-Bloch方程式
定常状態 =>
=>
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)

## Slide 81: Thermoelectricity: Boltzmann equation
太田英二、坂田亮著、半導体の電子物性光学、培風館 (2005)
Boltzmann-Bloch equation
: group velocity  : phase velocity
Steady-state
Non-uniform and chemical potential

## Slide 82: T dependence of mobility vs scat. mechanism
STOにおけるLOフォノン散乱には、主に〖ℏω〗_0= 99.0と 〖ℏω〗_0= 58.0 meVのエネルギーの高い2つのLOフォノン（LO3, LO2）が寄与しており[8][9]、エネルギーの低いLOフォノン(LO1)は殆ど寄与しない。
(a)
(b)
図 4‑18 x = 0.07のSTOH薄膜の移動度の温度依存性の実測値（赤丸）と (a)イオン化不純物散乱と音響フォノン散乱 (b)イオン化不純物散乱と光学フォノン散乱 を組み合わせたモデルによるフィッティング結果. （黒の実線）.
Notes: 82

## Slide 83: 熱電変換